## Slide 1: Phillips Metal Injection Molding
Skip Swanson
Manager
August 5, 2011

## Slide 2
Phillips Metal Injection Molding
Stout Technology Park Menomonie, WI
www.phillipsplastics.com
Notes: GREETING
BRIEF REVIEW OF TODAYS INTENT TO PROVIDE AN OVERVIEW OF THE METAL INJECTION MOLDING PROCESS.
PRESENTATION TIME : 30 MINUTES
REQUEST HOLDING QUESTIONS TO THE END OF THE PRESENTATION OR WRITING THEM IN THE WEB EX FIELD IN THE LOWER RIGHT OF YOUR SCREEN.

## Slide 3: Raw Material Mixing and Pellitization
Metal Powder
(-60% volume)
Polymer
Powder
(-40% volume)
MIM
Feedstock
Hot Mixer/Extruder
Process Keys:
Consistency of powder size distribution
Consistency of powder loading
Metal Powder
(-60% volume)
MIM
Feedstock
Hot Mixer/Extruder
Polymer
Powder
(-40% volume)

## Slide 4: Molding
Process Parameters:
High viscosity
High thermal
conductivity
Tool Temperatures –
250º F
Injection Molding Machine:
Advanced instrumentation
Closed loop control from pressure transducer to assure ultimate uniformity in molded part weight
Heater
Bands
Mold
Heater
Bands
Mold

## Slide 7
Custom Sintering Fixtures

## Slide 8: Catalytic Debinding
Process Parameters:
Chemical reaction
Shrinking core mechanism
Temperature is below
softening point of binder
Process Keys:
Fast (2-4 hours)
Clean
No distortion of parts
Exhaust Burner
Heater
Coils
Fan
s
Secondary
Binder
Shrinking Core Mechanism
Heater
Coils
Exhaust Burner
Secondary
Binder
Shrinking Core Mechanism
Fan
Catalyst

## Slide 9: Continuous Debind and Sintering
Process Parameters:
Temperature ramp to 1350° C
16-20 hour cycle door-to-door
Hydrogen or nitrogen
atmosphere
Sintered density 97-99%
of theoretical or wrought

## Slide 10
Continuous Debind and Sintering

## Slide 11: Continuous Debind and Sintering

## Slide 14: Endo Stitch program
The ENDO STITCH™ single use suturing device has application in endoscopic surgery for the placement of interrupted or running stitches in soft tissues.

## Slide 15: ENDO GIA Universal Stapler
Upper pivot
Retainer
Pivot

## Slide 16: Metal Injection Molding Design Examples
Parts previously were fine blanked and then three bosses assembled with screws
Significantly reduced component cost
MIM design eliminated a 7 piece assembly

## Slide 17
Auto-unscrewing Tools
Four cavity tool
0-80 auto-unscrewing thread
Eight cavity tool
M2 X 0.4 auto-unscrewing thread

## Slide 18: Educational Partenerships
UW – Stout
Chippewa Valley Technical College
UW - Eau Claire

## Slide 19: Educational Partenerships
UW – Stout
  Leadership Academy
  Lean Manufacturing Training
  Scientific Injection Molding Training
  Industrial Technology graduates
    Plastics Engineering
    Manaufacturing Engineering
    Product Development
  People Process
  Technical Interns
  Continuing Education

## Slide 20: Educational Partenerships
Chippew Valley Technical College
  Electro Mechnical Education
  Computer Software Training
  Precision Inspection
  Geometric Dimensioning and Tolerancing
  Blueprint Reading
  Negotiating Skills

## Slide 21: Educational Partenerships
UW-Eau Claire
  MBA Program
  Leadership Training
  Scanning Electron Microscope
    Contour Observation
    Fracture Analysis
    Energy Spectrum Probe
    Grain Boundary Analysis

## Slide 22: Thank You!
www.phillipsplastics.com